## Slide 1: Determination of Viscosity Average Molecular Weight of Polymer
Experiment 1:

## Slide 2
Objective:
Determine the absolute viscosity of Polymer solutions of different concentrations
Determine the viscosity average molecular weight of a polymer.

## Slide 3: Methods of Molecular Weight Determination
Number Average Molecular Weight
  End-group analysis
  determine the number of end-groups in a sample of known mass
  Colligative Properties
  most commonly osmotic pressure, but includes boiling point elevation and
  freezing point depression
Weight Average Molecular Weight
  Light scattering
  translate the distribution of scattered light intensity created by a dissolved
  polymer sample into an absolute measure of weight-average MW
Viscosity Average Molecular Weight
  Viscometry
  the viscosity of an infinitely dilute polymer solution relative to the solvent
  relates to molecular dimension and weight.
Molecular Weight Distribution
  Gel permeation chromatography
  fractionation on the basis of chain aggregate dimension in solution
Z-average Molecular Weight
Centrifuge
average determined by centrifuge

## Slide 4: Polymer Solution Viscosity
When a polymer is dissolved in a solvent and then subjected to flow through a narrow capillary it exerts a resistance to that flow. This resistance is very informative.
It provides information on the size of the polymer
Its Flexibility and shape in solution
Its interactions with the solvent it is disolved in.
Notes: A characteristic feature of a dilute polymer solution is that its viscosity is considerably higher than that of either the pure solvent or similar dilute solutions of small molecules. This arises due to the large difference in size between polymer and solvent molecules, and the magnitude of the viscosity increase is related to the dimensions of the polymer molecules in solution. Therefore, measurements of the viscosities of dilute polymer solutions can be used to provide information are polymer structures, molecular shapes, D.P. and polymer solvent interactions. However, it is mainly used to determine molecular weight.
For a dilute polymer solution, the ratio between flow time of a polymer solution (t) to that of the pure solvent (to) is effectively equal to the ratio of their viscosities - or “relative viscosity”.
As this has a limiting value of unity, i.e.  = o , a more useful quantity is specific viscosity (sp ) such that

## Slide 5: Polymer Solution Viscosity
For dilute solutions the ratio between flow time of a polymer solution (t) to that of the pure solvent (to) is effectively equal to the ratio of their viscosity (h / ho)
As this has a limiting value of unity, a more useful quantity is specific viscosity (hsp)
Notes: A characteristic feature of a dilute polymer solution is that its viscosity is considerably higher than that of either the pure solvent or similar dilute solutions of small molecules. This arises due to the large difference in size between polymer and solvent molecules, and the magnitude of the viscosity increase is related to the dimensions of the polymer molecules in solution. Therefore, measurements of the viscosities of dilute polymer solutions can be used to provide information are polymer structures, molecular shapes, D.P. and polymer solvent interactions. However, it is mainly used to determine molecular weight.
For a dilute polymer solution, the ratio between flow time of a polymer solution (t) to that of the pure solvent (to) is effectively equal to the ratio of their viscosities - or “relative viscosity”.
As this has a limiting value of unity, i.e.  = o , a more useful quantity is specific viscosity (sp ) such that

## Slide 6: Intrinsic Viscosity [η]
To eliminate concentration effects, the specific viscosity (hsp ) is divided by concentration and extrapolated to zero concentration to give intrinsic viscosity [h]
Thus plotting hsp/c vs c, the intercept is the intrinsic viscosity [h] and from the slope, KH (Huggins constant, typically between 0.3 - 0.9) can be determined
Notes: To eliminate concentration effects (although minimal if existent in dilute solution), the specific viscosity is divided by concentration and extrapolation to zero concentration to yield Intrinsic viscosity [ ].
Thus plotting solution viscosity () minus the solvent viscosity (o) divided by the solvent viscosity (o) multiplied by polymer concentration will provide Intrinsic viscosity [ ] (y-intercept) and KH (Huggins constant) from the slope.
The following example demonstrates this.

## Slide 7
Determination of Molecular Weight
The concentration dependence is observed to follow this functional dependence:
Neglect higher order term in c.
Plot of hsp/c vs c will yield [h] as y-intercept.
k = Huggins constant
k=2 for rigid uncharged spheres
k=0.35 for flexible polymers
y-intercept
Viscosity Average Molecular Weight
  Viscometry

## Slide 8
From the Mark-Houwink equation the relationship among the molecular weight and viscosity are given below
[η] = K Mα
Where η is the intrinsic viscosity,М is Molecular weight, Κ and α are constants for a particular polymer solvent system. If we know the Κ and α values for a given polymer solution the intrinsic viscosity and molecular weight can be calculate using the above equation.

## Slide 9: Intrinsic Viscosity Determination
0.2
0.4
0.6
0.8
1.0
C (g dl-1)
2.0
2.5
3.0
3.5




[h]
KH[η2]
Notes: From the flow times in a capillary viscometer for a dilute polymer-solvent system, the intrinsic viscosity [] and Huggins constant KH can be determined.
The y-intercept (2.18) is the corresponding intrinsic viscosity [], thus enabling the determination of the Huggins constant by dividing the slope by the square of the intrinsic viscosity ( ).

## Slide 10
Intrinsic viscosity [h] can be related to molecular weight by the Mark-Houwink-Sakurada Equation
Applicable for a given polymer-solvent system at a given temperature
Viscosity-Molecular Weight Relations
Log [h] vs log M (w or n) for a series of fractionated polymers produces log K (intercept) and a (slope)
A wide range of values have been published
  a ~ 0.5 (randomly coiled polymers)
  ~ 0.8 (rod-like, extended chain polymers)
  K between 10-3 and 0.5
Notes: Intrinsic Viscosity [] is the most useful of the various viscosity designations because it can be related to molecular weight by the Mark-Houwink-Sakarada equation
where Mv is the viscosity average molecular weight. The constants K and a are the intercept and slope respectively, of a plot of log [] versus log Mw or Mn of a series of fractionated polymer samples. Such plots are linear (except at low molecular weight) for linear polymers.
As a result, a wide range of constants K and a have been published.

## Slide 11
Experiment 6: Determination of capacity of Resin (Ion Exchange)
Chemistry & Background Attached to the carbon skeleton of the resin are the active groups that bind the exchangeable ions. Initially, the cation exchange resin used in this experiment is in the hydrogen ion form, in which H+ ions are bound to the active sites.

## Slide 13
If a salt solution is passed through the ion exchanger, however, hydrogen ions can be easily lost into the solution in exchange for cations from the dissolved salt. When the exchange occurs, the electrical neutrality of the resin is maintained. This exchange process is shown in the following equation:

## Slide 14
A convenient notation for representing the stoichiometry of ion exchange processes uses the notation RSO3H to represent a single active group, with R to representing the inert resin it is attached to thus, the previous process
becomes
RSO3H + Na+ + H2O (RSO3-)(Na+) + H3O+
If the absorbed cation has a +2 charge, two hydrogen ions are displaced. For a dipositive cation (such as Mg2+), we write
2 RSO3H + Mg2+ + 2 H2O (RSO3-)2(Mg2+) + 2 H3O+

## Slide 15
Procedure:
1) Regenerate the column with 0.1 M HCl (rinse 2 times)
2) Rinse the column with reagent grade water (test for chloride or protons)
3) Quantitatively transfer a known amount of NaCl of a known NaCl solution to the column. Collecting column eluent. Rinse the column three times with water also collecting the eluent.
4) Titrate the H+ in eluent solution obtained in step three with NaOH. You may use a pH or conductivity probe to follow the titration.
5) Repeat this procedure three times.

## Slide 16
Ml NaOH X MNaOH X A.wt Na
Capacity = -----------------------------------------
massresin

## Slide 17
Experiments: Determination of specific volume of polymer by refractive index method
Specific volume is a property of materials, defined as the number of cubic meters occupied by one kilogram of a particular substance. The standard unit is the meter cubed per kilogram (m3/kg or m3·kg−1).
Specific volume is inversely proportional to density. If the density of a substance doubles, its specific volume, as expressed in the same base units, is cut in half. If the density drops to 1/10 its former value, the specific volume, as expressed in the same base units, increases by a factor of 10.

## Slide 18
The specific volume of the polymer is calculated using the following equation:
n1 = n2 –(1/V2). (dn/dc)
The slope of the curve = (1/V2)
V2 = 1/slope

## Slide 19
Concentration | nº | n1 | dn | dn/dc
%0 |  |  |  | 
%6 |  |  |  | 
%3 |  |  |  | 
%1.5 |  |  |  | 

## Slide 20: Preparation of polyether-sulfone by Interfacial polymerization by using PTC.
The nucleophilic polycondensation has the advantage that the chemical structure and thus the properties of the poly(ether sulfone)s can be varied in a relatively simple way through the selection of the bisphenol components.The technically most important poly(arylene ether sulfone) is obtained from bisphenol A and 4,4'-dichlorodiphenyl sulfone by nucleophilic aromatic
polysubstitution.