## Slide 1
Strength of materials lab.
Second year student 2017-2018
Why are metals tested ?
Ensure quality
Test properties
Prevent failure in use
Make informed choices in using materials
Factor of Safety is the ratio comparing the actual stress on a material and the safe useable stress.
Two forms of testing
Mechanical tests – the material may be physically tested to destruction. Will normally specify a value for properties such as strength, hardness, toughness, etc.
Non-destructive tests (NDT) – samples or finished articles are tested before being used

## Slide 2
STRENGTH OF MATERIALS LABORATORY – SYLLABUS
1. Tension test .
2. Compression test
3. Torsion test .
4. Impact test on metal specimen
5. Creep test on lead.
6. Hardness test on metals – Brinnell.on UTM
7. Deflection test on Cantilever beam .
8. Deflection test on simply supported beam
9. Photoelasticity .
10.Fatigue test
INSTRUCTIONS
1. Students should report to the labs concerned as per the timetable.
2. Record should be updated from time to time and the previous experiment must be signed by the faculty in charge concerned before attending the lab.
3. Students who turn up late to the labs will in no case be permitted to perform the experiment scheduled for the day.
4. After completion of the experiment, certification of the staff in-charge concerned in the observation book is necessary.
5.The record of observations along with the detailed experimental procedure of the experiment performed in the immediate previous session should be submitted and certified by the staff member in-charge.

## Slide 3
Tensile Test - Introduction
The tensile test is a common test performed on metals, wood, plastics, and most other materials.
Tensile loads are those that tend to pull the specimen apart, putting the specimen in tension. They can be performed on any specimen of known cross-sectional area and gage length to which a uniform tensile load can be applied.
Tensile tests are used to determine the mechanical behavior of materials under static, axial tensile, or stretch loading.
ASTM standards for common tensile tests may be found in sections E8 (metals), D638 (plastics), D2343 (fibers), D897 (adhesives), D987 (paper), and D412 (rubber).
UltimateTensile Strength - The maximum tensile stress that a material is capable of developing during a test.
Load- Applied force either pounds or newtons
Stress - The intensity of the internally-distributed forces or components of forces that resist a change in the form of a body. Commonly measured in units dealing with force per unit area, such as pounds per square inch (PSI or lb/in2) or Megapascals (Mpa). The three basic types of stress are tension, compression, and shear. The first two, tension and compression, are called direct stresses.

## Slide 4
Elastic Limit - The greatest amount of stress a material can develop without taking a permanent set.
Percent Elongation - The total percent strain that a specimen develops during testing.
Principal properties determined through tensile testing include yield strength, tensile strength, ductility (based on the percent elongation and percent reduction in area), modulus of elasticity, and visual characteristics of the fracture. For brittle materials, which do not show a marked yield or ductility, data is collected for tensile strength and type and condition of fracture.
Expected Results
The results of tensile testing can be used to plot a stress-strain curve which illustrates the tensile properties of the material. Stress (in pounds per square inch or Pascal's) is plotted on the vertical axis while strain (inches per inch, millimeters per millimeter, or unit less) is plotted along the horizontal.
As the load is applied, the curve is proportional and this period of linearity is termed the elastic region. Once the curve deviates from a straight line and begins to yield, the material has reached the proportional limit. Once the material has yielded, it exhibits plastic behavior or plasticity. Brittle materials do not exhibit much yield and are, therefore, less curved than ductile materials.

## Slide 5
Modulus of Elasticity - Also known as Young’s modulus; calculated by finding the slope of the stress-strain curve for a given material within the range of its linear proportionality between stress and strain.
Proportional Limit - The greatest stress a material can develop without deviating from linearity between stress and strain. Otherwise stated, the greatest stress developed in a material within its elastic range.
Percent Reduction in Area - The difference between the original and final cross-sectional areas of a test piece, expressed as a percentage.
Yield Point – Also referred to as Elastic Limit, is the point at which any additional stress will result in permanent deformation.
Yield Strength - The stress at which a material exhibits a specified limiting permanent set.

## Slide 6
The engineering stress is:
P is the load in lbs. on the specimen and A0 is the original cross-sectional area near the center of the specimen.
On the other hand, the true stress is the load divided by the true area, which continues to be smaller by the tensile load.
The true stress continues to increase to the point of fracture, while the engineering stress decreases to the point of fracture due to the increasing load and the constant cross-sectional area.
The engineering strain is:
l is the gage length at a given load and l0 is the original gage length with zero load
Modulus of Elasticity E
The slope of the stress-strain curve in the elastic deformation region is the modulus of elasticity, which is known as Young's modulus

## Slide 10
Compression Testing - Introduction
Simplistically, compression testing is the opposite of tensile testing. A compressive load tends to squeeze or compact the specimen. The choice of a compression test over other types of testing largely depends on the type of loading the material will see during application or service.
Metals and many plastics, for example, are more efficient at resisting tensile loads. Therefore, they are more commonly tested using tensile loading, depending on the application, of course. Materials, such as concrete, brick, and some ceramic products, are more often used in applications for their compressive loading properties and are, therefore, tested in compression. Again, it is important to choose the test that best reflects the loads and conditions the material will be subjected to in application or service.
Compression Testing – Procedure
During a typical compression test, data are collected regarding the applied load, resultant deformation or deflection, and condition of the specimen. For brittle materials, the compressive strength is relatively easy to obtain, showing marked failure. However, for ductile materials, the compressive strength is generally based on an arbitrary deformation value. Ductile materials do not exhibit the sudden fractures that brittle materials present. They tend to buckle and "barrel out".

## Slide 11
Prior to this and any test, the dimensions of the specimen should be measured with adequate precision using proper instruments. Once these measurements have been taken and recorded, the specimen should be loaded into the testing machine.
In compression testing, and testing in general, care should be taken to insure that the axis of the specimen is centered and aligned with the axis of loading.
Loading rates should be steady and continuous. Rates vary, but a general figure is 0.005 inches per minute strain rate. Loading rates typically range from 500-1000 lb/min.
As in most tests of mechanical properties, the loading rate can adversely affect the results if you get carried away. Loading continues at this rate up to approximately one-half of the anticipated strength and, then, should be reduced to allow for more frequent data collection. In this way, subtle changes can be observed in the specimen's behavior.
As in all of these tests, please observe proper safety procedures. Obtain and properly wear personal protective equipment. Some of these materials exhibit violent fractures with explosive results.

## Slide 12
Impact Testing – Introduction
A specimen under test will exhibit different properties, depending on the rate at which the load is applied. For example, most materials will exhibit greater strength is the load is applied in a slower, gentler manner (static loading) than suddenly (dynamic). Because properties are strain-rate dependent, tests have been standardized to determine the energy required to break materials used sudden blows. These are termed impact tests.
Impact tests generally involve sudden shock loading that results in breakage of the specimen. The result is calculated based on the energy required to break the specimen and the resultant loss of momentum. This can be calculated if one knows the initial energy and final energy or the initial angle and final angle of the object used to break the specimen. The Izod and Charpy tests are commonly used to measure impact strength. They differ only slightly, the configuration and specifications of the test specimen.